Status and Outlook of Sensitizers/Dyes Used in Dye Sensitized Solar Cells (DSSC): A Review

S Shalini a,*, R Balasundaraprabhu a, T Satish Kumar b, N Prabavathy a, S Senthilarasu c,                 S Prasanna a

a Centre for sustainable photovoltaic technology, Department of Physics, PSG College of Technology, Coimbatore – 641004, Tamil Nadu, India

b Department of Metallurgical Engineering, PSG College of Technology, Coimbatore – 641004, Tamil Nadu, India

c Environment and Sustainability Institute, University of Exeter, Penryn, Cornwall TR10 9EZ, United Kingdom

*Corresponding author. Tel: 0422-4344535 E-mail address: shalini1689@gmail.com

Abstract: Dye sensitized solar cells (DSSC) have become a topic of significant research in the last two decades because of their scientific importance in the area of energy conversion. Currently DSSC is using inorganic Ruthenium (Ru)-based, metal-free and natural dyes as sensitizer. The use of metal free and natural dyes have become a viable alternative to expensive and rare Ru-based dyes because of low cost, ease of preparation, easy attainability and environmental friendliness. Most of the alternatives to Ru-based dyes have so far proved inferior to the Ru-based dyes because of their narrow absorption bands (Δλ≈100-250 nm), adverse dye aggregation and instability. This review highlights the recent research on sensitizers for DSSC, including Ru-complex dyes, metal-free dyes and natural dyes. It also details and tabulates all types of sensitizer with their corresponding efficiencies. Plot of progress in efficiency(η) of DSSC till date based on three types of sensitizers is also presented.

Keywords: Dye sensitized solar cells; TiO2 film; Ru-based dyes; Metal free dyes; Natural dyes; Stability.

1.  Introduction

Following the important and novel contribution on dye-sensitized solar cells (DSSC) by Grätzel et al in 1991 [1], several reports have been published considering DSSC as an efficient low cost alternative for the conventional solar cells [1-2]. A DSSC presents three important steps to convert sunlight into electrical energy: It relies on the visibile photo-excitation of dyes triggering an electron transfer into the conduction band of the metal oxide semiconductor (generally TiO2), followed by regeneration of the oxidized dye molecules by the electron donation from the redox couple in the electrolyte, and finally migration of electron through the external load to complete the circuit [3, 4]. The entire operation takes place with the help of different components of DSSC, such as the light-absorber (dye/sensitizer), the electron-transport agent (wide band-gap nanocrystalline semiconductor), and the hole-transport agent (redox couple in electrolyte) [5, 6].

Moreover in order for a DSSC to be successful, all the components constituting the system should effectively play their role. Sensitizer/dye in particular should possess certain important features for efficient performance, namely, a broad and strong absorption from visible to near infra red region [7-9], chemical stability of the appropriate LUMO and HOMO levels for effective charge injection into the semiconductor [10, 11] and dye regeneration from the electrolyte, high molar extinction coefficients in the visible and near-infrared region for light-harvesting, good photostability and solubility to hamper the recombination [12,13].

The most successful sensitizers in terms of efficiency and stability are based on Ru- bipyridyl compounds. Moreover, these dyes are also having advantageous characteristics such as excellent stability, higher absorption in the visible range of solar spectrum; excellent electron injection and efficient metal-to-ligand charge transfer [14-16]. Even though Ru based dyes are capable of yielding conversion efficiencies greater than 10 %, their preparation normally requires multi-step procedures and time consuming chromatographic methods [17, 18].

Other issues in considering Ru based dyes are their cost as Ru is a rare metal with a high price and its toxic nature. They also possess low molar extinction coefficients and restricted NIR absorption [4]. However, efficient Ru-free sensitizers that could also lead to an efficient light harvesting with a decrease in total cell cost are also studied [19]. Thus, research into Ru free dyes, including metal-free organic dyes and metal-complex porphyin dyes, has intensified because of the high cost of Ru metal [20].

On the other hand, natural dyes have also been studied widely for usage as DSSC sensitizer because of their large absorption coefficients in visible region, relative abundance, ease of preparation and environmental friendliness [21, 22]. Most importantly, the synthesis route for natural dye based DSSC is cost effective as it does not involve noble metals like Ru. Despite the availability and low cost of natural dyes, most of them do not yield energy conversion efficiencies of over 2 %, although some natural dyes derivatives are capable of higher energy conversion efficiencies [23].

To the best of our knowledge, there are only limited review articles that details on different types of sensitizers employed in DSSC [15, 23]. This review article exclusively highlights and discusses the recent research and advances on sensitizers/dyes for DSSC, including Ru-complex dyes, metal-free organic dyes, metal-complex porphyin dyes, and natural dyes. The different sensitizers used for DSSC is explained in the view of considering the DSSC operating with iodine based electrolytes, as it is today impossible to disconnect dyes and electrolytes. It also details and tabulates all the types of sensitizer with their corresponding efficiencies. Plot of progress in efficiency (η) of DSSC till date based on three different types of sensitizers is also presented.

2. Requirements for efficient performance of a sensitizer

The role of a sensitizer in DSSC is to as a molecular electron pump. It helps in absorbing the visible light, pumping an electron into the conduction band of TiO2 layer, accepting an electron from the redox couple, and then repeating the cycle [24, 25]. A sensitizer should possess certain peculiar characteristics such as (1) strong absorption in the visible range (2) high stability in the oxidized, ground and excited states (3) suitable redox potential (4) good efficiency in the charge injection and regeneration processes. Few important characteristics of a sensitizer are discussed below. All the reactions that occur inside a DSSC with HOMO-LUMO energy levels and with the corresponding electrical potential vs SHE (standard hydrogen electrode) are schematically represented in Figure 1.

Fig.1 Schematic of all reactions that occur inside a DSSC with HOMO-LUMO energy levels and with corresponding electrical potential vs SHE (standard hydrogen electrode)

2.1. Absorption spectrum

Concentration of the dye within the nanoporous TiO2 surface and the absorption coefficient determines the fraction of light that is absorbed by the TiO2 layer [12]. A sensitizer should possess a high absorption coefficient in the visible region and a high affinity to the TiO2 surface in order to ensure a dense coverage of the surface [26]. Also increase in absorbance helps in reducing the thickness of the TiO2 layer thereby decreasing the recombination probability [12, 26].

Generally at longer wavelengths, the absorption decreases significantly, thus a substantial fraction of the solar spectrum will be lost. The absorption of the dye can be described with Beer-Lambert's Law (Equation 1) [12, 27, 28]

I(x)I0=10-αλ*x*Cdye									(1)
 where I(x) is the light intensity at the point x (Wm-2)

I0 is the initial light intensity (Wm-2)

α is the absorption coefficient (M-1cm-1)

λ is the wavelength (nm)

cdye is the concentration of the dye (M)

x is the path length (cm)

2.2 Attachment groups

When the semiconductor oxide film is exposed to the dye solution, the attachment group of the dye helps to form a monomolecular layer. This molecular layer ensures a high probability of relaxation of the excited dye molecules into the semiconductor conduction band by electron injection. A common anchoring group is carboxylate group which can form an ester bond with the TiO2 surface, allowing facile electronic communication [29-31].

2.3. Energy level

In order to ensure efficient charge injection, the difference between the LUMO and HOMO level of the excited dye molecule should be in the order of 0.2-0.3 eV above the conduction band of the TiO2 [32, 33]. In this case the activation energy for reduction of the oxidized sensitizer by a TiO2 conduction band electron (back reaction) increases and the corresponding rate constant becomes very less to compete with the dye regeneration by the electrolyte.

The energy level of the dye, especially at high dye coverage can be shifted if the dye agglomerates on the surface of the TiO2. High dye coverage refers to effective intermolecular interactions with no back-electron transfer. This shift may result in different electronic properties of the ground state and/or the excited state, which generally affects the charge injection efficiency [34, 35].

2.4. Charge injection and charge recombination

Charge injection generally occurs from the π*-orbital of the anchoring group to the titanium 3d-orbital. An efficient charge injection can be ensured only when these orbitals overlap each other. Injection of electrons from the dye to the conduction band (CB) of TiO2 happens in a femtosecond (fs) to picosecond (ps) time scale whereas charge recombination takes place in the micro to millisecond time scale [12, 36]. The equation for charge injection and charge recombination is given in Equation 2 and Equation 3 respectively.

(2)

(3)

A prerequisite for an efficient charge injection is that the back reaction of a TiO2 conduction band electron to the oxidized dye should be much slower than the reduction of the oxidized dye by the electrolyte. Similarly, charge injection can occur either from the singlet or the triplet state. The rate of a reaction (rate constant) for injection differs as electron is injected from either singlet or triplet state. The rate constant for injection in both the cases is on a time scale of less than 100 fs [37, 38].

2.5. Stability

Any sensitizer in a DSSC has to sustain and should not have significant degradation at least for twenty years of operation and should sustain natural light for this period of time [39]. Ideally, the electron injection and electron regeneration is completely reversible. However, in any real device, some degradation of the dye occurs. The rate constant for decomposition (k) is given by the following equation [38, 39]

(4)

where k is the rate constant for degradation from the ground state (s-1)

cdye,0 is the initial dye concentration (M)

cdye,lifetime is the dye concentration at some time ‘t’(M)

lifetime is the lifetime of the cell (example: 20 years ≈ 6.3*108 s)

Under illumination, degradation occurs from the excited state dye* or from the oxidized state dye+. Since the injection from dye* state is ultrafast, it is believed that light induced degradation mainly occurs from the state dye+. The irreversible degradation of the oxidized dye molecule competes with the regeneration by the electrolyte (rate constant k) and is represented by the Equation 5 [12, 29].

(5)

where I- is the iodide concentration (M)

3. Recent developments in DSSC sensitizers

Tremendous attempts have been made for developing different sensitizers which can be broadly divided into the following three types

- Ru-complex dyes

- Organic dyes

- Natural dyes

3.1. Ru-complex dyes

In 1991, Ru-based DSSC showed a remarkable success with a conversion efficiency of 7.1% [1]. Ru (II) metal is always a good choice of study for a number of reasons: (1) its octahedral geometrical structure tolerate extending of specific ligands in a controlled manner; [40] (2) the photophysical, photochemical and electrochemical properties of Ru (II) complexes can be tuned; (3) it possesses stable and accessible oxidation states from I to IV [40, 41]; (4) possess good solubility in many solvents [12].

Further in 1993, DSSC with a conversion efficiency of 10.3 % was reported by Nazeeruddin et al [40], using Ru dye (N3 dye) as sensitizer (N3-cis-di (thiocyanato) bis (2, 2-bipyridine-4, 4-dicarboxylate) ruthenium). In 2001, Nazeeruddin et al. reported DSSC with 10.4% efficiency using a Ru dye called ‘black dye’ [42] and in 2006 reported a new dye called N179 (di-tetrabutyl ammonium cis-bis (isothiocyanato) bis (2, 2′-bipyridyl-4, 4′-dicarboxylato) ruthenium (II)) which was similar to N3, but resulted in a conversion efficiency of 11.2% [43].

Generally Ru dyes are classified as carboxylate polypyridyl Ru dyes, phosphonate Ru dyes and polynuclear bipyridyl Ru dyes. The main difference between the first two types lies in their adsorption groups. Whereas, the first two types of sensitizers differ from the third one by the number of metal centres present in their structure [44].

N3 dye in its structure possesses two bipyridine and two isothiocyanato (NCS) ligands. The chemical structure of N3 dye is shown Figure 2a. It absorbs up to 800 nm radiation due to the loosely-attached NCS groups [44]. The light absorption by the dye is attributed to the transition metal-to ligand charge transfer (MLCT) and the molecular orbitals HOMO and LUMO. The isothiocyanato ligands are the chromophore of the molecule and they shift the HOMO level negatively towards a red shift in its absorbtion spectra [29, 40].

Changing the protonation of the acid groups has been found to be a successful improvement to the dye structure that can lead to the synthesis of N719 dye. N719 dye has the same structure as N3 dye but has TBA+ (tetrabutyl ammonium) instead of H+ at two carboxyl groups and has been so far the most successful dye for DSSC [29, 30, 44]. The chemical structure of N719 dye is shown Figure 2b.

Fig.2 Chemical structures of Ru complexes (a) N3 dye (b) N719 dye (c) black dye

N749 dye (black dye), absorbs up to 860 nm of radiation and showed performance similar to that of N3 and N719 dyes. The chemical structure of black dye is shown Figure 2c. However, the absorption coefficient of N749 is lower than N3 and N719 dyes. Lower absorption coefficients usually require thicker metal semiconductor oxide electrodes to adsorb more dye molecules [29, 44]. Disadvantages in increasing the thickness of the metal semiconductor oxide layer lies in the view of electron transport, that is, it could lead to decrease in short circuit current density and open circuit voltage [45].

3.2. Metal free dyes

Metal free dyes are desired in the last years and the current application of these dyes for usage in DSSC has increased and is comparable to that of Ru-based sensitizers [29, 46]. The advantages of choosing metal free dyes as an alternative for Ru-based complexes are their very high molar extinction coefficients, free form expensive and toxic Ru metal, facile synthesis, easily tunable absorption energies, low cost and stability under elevated temperature and/or prolonged illumination [12, 29].

Metal free dyes are generally divided in three major parts in terms of molecular structure such as donors, linkers and acceptors. Linkers are usually π-conjugated system that link electron-donating (D) and electron-accepting (A) groups by bridges; so-called D-π-A sensitizers [47, 48]. In order to increase the conversion efficiency, the structure of these dyes needs to be altered [20, 29]. This can be achieved by extending the π-conjugation of the linkers and increasing the electron-donating and electron-accepting capability of donors and acceptors. Moreover, aggregation of dye molecules on TiO2 surface should be avoided although a controlled aggregation could be considered beneficial. This problem can be avoided by incorporating long alkyl chains and aromatic groups into the dye structure [49].

There are many classes of organic sensitizers that have been studied for the application in DSSC. The most promising metal free dye classes at the moment are coumarin dyes, porphyin dyes and indoline dyes [12, 49].

3.2.1. Coumarin dyes

Coumarin is a natural chemical compound found in many plants. The first coumarin dye was named as C343 and was demonstrated by Kay and Gratzel in 1996 [50] and found fast injection rates of 200 fs from dye into the conduction band of TiO2 [12, 20, 29]. The chemical structure of C343 dye complex is shown Figure 3a. Since C343 has a narrow absorption spectrum, the conversion efficiency of this specific compound was found to be low. Addition of more methane groups can help in expanding the π-conjugation linkers and thereby helps in increasing the efficiency of the DSSC [49].

Fig.3 Chemical structures of Metal free dyes (a) coumarin dye (b) porphyrin dye (c) indoline dye

3.2.2. Porphyin dyes

Another class of metal free dyes is porphyin dyes or porphyins. Porphyins are characterized by four modified pyrrole subunits interconnected via methane bridges (=CH-). The chemical structure of porphyin dye complex is shown Figure 3b. This structure resembles a high π-conjugated system with very intense absorption in the visible region and with high extinction coefficient [20, 29]. Moreover, porphyins have a long life time in its excited singlet state (> 1 ns), very fast electron injection rate (fs range), milli second time scale electron recombination rate and tunable redox potentials [20].

3.2.3. Indoline dyes

Indole has a bicyclic structure, consisting of a six-membered benzene ring combined to a five-membered nitrogen-containing pyrrole ring [51]. The chemical structure of indole is shown Figure 3c. To date, these indole based dyes have a great potential as sensitizers. Structure of this dye consists of an electron withdrawing anchoring group on the benzene ring and an electron donating group on the nitrogen atom [52].

Generally the indole moiety acts as electron donor and is connected to a rhodanine group which act as electron acceptor. Furthermore, the absorbance in the IR region of the visible spectra and the absorption coefficient of the dye can be greatly enhanced by introducing aromatic units into the core of the indoline structure [20, 52].

Table 1 summarizes the photo electrochemical parameters of various Ru-based dye sensitizers.

Table 1 Photo electrochemical parameters of Ruthenium based and metal free sensitizers

| Dye | Jsc (mA/cm2) | Voc (V) | FF | η (%) | Ref |
| --- | --- | --- | --- | --- | --- |
| N3 | 18.2 | 0.72 | 0.73 | 10 | [53] |
| N719 | 17.73 | 0.84 | 0.75 | 11.18 | [54] |
| Black dye | 20.5 | 0.72 | 0.704 | 10.4 | [55] |
| Black dye | 20.9 | 0.73 | 0.722 | 11.1 | [56] |
| Z907 | 13.6 | 0.72 | 0.692 | 6.8 | [57] |
| Z907 | 14.6 | 0.72 | 0.693 | 7.3 |  |
| K8 | 18 | 0.64 | 0.75 | 8.64 | [58] |
| K19 | 14.61 | 0.71 | 0.671 | 7 |  |
| N945 | 16.5 | 0.79 | 0.72 | 9.6 | [59] |
| Z910 | 17.2 | 0.77 | 0.764 | 10.2 | [60] |
| K73 | 17.22 | 0.74 | 0.694 | 9 | [61] |
| K51 | 15.4 | 0.73 | 0.685 | 7.8 |  |
| C343 | 14 | 0.6 | 0.71 | 6 | [62] |
| Porphyin based | 3.76 | 0.54 | 0.67 | 1.4 | [63] |
|  | 2.63 | 0.61 | 0.71 | 1.2 |  |
|  | 5.79 | 0.61 | 0.66 | 2.4 |  |
| Indoline | 18 | 0.69 | 0.78 | 9.4 | [64] |

3.3. Natural dyes

Naturally available fruits, flowers, leave, bacteria etc exhibit various colors and contain several pigments that can be easily extracted and employed in DSSC [65]. Advantages of employing these natural dyes in DSSC are their large absorption coefficients in visible region, relative abundance, ease of preparation and environmental friendliness [16, 17]. Most importantly, the synthesis route for natural dye based DSSC is cost effective as it does not involve noble metals like Ru. [18].

These plant pigments exhibit electronic structure that interacts with sunlight and alters the wavelengths that are either transmitted or reflected by the plant tissue. This process leads to the occurrence of plant pigmentation and each pigment is described from the wavelength of maximum absorbance (λmax) and the color perceived by humans [66]. Pigments for natural dyes include chlorophyll, carotenoid, flavonoid and anthocyanin that are relatively easy to extract from natural products when compared to synthetic dyes [67].

3.3.1. Chlorophylls

Chlorophylls belong to natural photosynthetic pigments [68, 69] which give plants green color. The two major types of chlorophylls are chlorophyll ‘a’ and chlorophyll ‘b’. Chlorophylls and their derivatives are employed as sensitizers in DSSC because of their tendency to absorb blue and red light. The most efficient is the derivative of chlorophyll ‘a’ (methyl trans-32-carboxy-pyropheophorbide) [66]. The absorbance spectrum of chlorophyll ‘b’ shows a characteristic blue tinge and has a redshift when compared to chlorophyll ‘a’. Chemical structure of Chlorophyll ‘a’ and Chlorophyll ‘b’ is shown in Figure 4a.

Fig.4 Chemical structures of Natural dye pigments (a) chlorophyll (b) flavonoid (c) anthocyanin (d) carotenoid

3.3.2. Flavonoids

Flavonoids are the most widespread and physiologically active group of natural constituents with a basic C6-C3-C6 skeleton. Flavone consists of two benzene rings, joined together by a γ ring that distinguishes one flavonoid compound from the other [66]. Figure 4b shows the basic chemical structure of commonly occurring flavonoid.

In case of flavonoids, the charge transfer transitions from HOMO to LUMO require lesser energy, energizing the pigment molecules by visible light, leading to a broad absorption band in the visible region. This flavonoid gets rapidly adsorbed to the surface of TiO2 by displacing an OH– counter ion from the Ti (IV) site that combines with a proton which is donated by the flavonoid [18, 70].

3.3.3. Anthocyanins

Anthocyanins are glycoside salts of phenyl-2-benzopyrilium based on a C15 skeleton with a chromane ring bearing a second aromatic ring B in position 2 (C6-C3-C6) [71, 72]. Basic chemical structure of anthocyanin is shown in Figure 4c.

Anthocyanins are responsible for existence of attractive colors, from scarlet to blue, of flowers, fruits, leaves etc and are also identified in mosses and ferns [73]. Anthocyanins are also responsible for modifying the quantity and quality of light that is incident on the chloroplasts [74]. Anthocyanin molecules have carbonyl and hydroxyl groups bound to the surface of TiO2 semiconductor, which helps in excitation and transfer of electrons from the anthocyanin molecules to the conduction band of porous TiO2 film [18]. The bonding between the functional groups such as carbonyl and hydroxyl groups with TiO2 surface is schematically presented in the Figure 5.

Fig.5 The Schematic representation of the bonding between carbonyl and hydroxyl groups with the surface of TiO2

3.3.4. Carotenoids

Carotenoids are a large family (over 600 members) of isoprenoids that provide many fruits and flowers with distinctive red, orange and yellow colors. Carotenoids are distinguished by the presence of C40 hydrocarbon backbone which induces structural and oxygenic modifications [66]. Figure 4d shows the chemical structure of carotenoid. The light absorption is achieved by a photo induced transformation of ‘p’ delocalized electrons of carotenoid molecules. This in turn transfers the absorbed energy to the chlorophyll molecules to form a singlet chlorophyll state with a slightly higher energy. This transfer of energy from carotenoids to chlorophyll molecules is facilitated by physical structure of chlorophyll [75].

Table 2 summarizes the photoelectrochemical parameters of the different natural dyes extracted from leaves, seeds, flowers, fruits, vegetables and tree barks.

Table 2 Photoelectrochemical parameters of the natural dyes extracted from leaves, seeds, flowers, fruits, vegetables and tree barks

| Dye Solution | Jsc (mA/cm2) | Voc (V) | FF | η (%) | Ref |
| --- | --- | --- | --- | --- | --- |
| Begonia | 0.63 | 0.537 | 72.2 | 0.24 | [76] |
| Tangerine Peel | 0.74 | 0.592 | 63.1 | 0.28 |  |
| Rhododendron | 1.61 | 0.585 | 60.9 | 0.57 |  |
| Fructus Lycii | 0.53 | 0.689 | 46.6 | 0.17 |  |
| Marigold | 0.51 | 0.542 | 83.1 | 0.23 |  |
| Flowery Knotweed | 0.60 | 0.554 | 62.7 | 0.21 |  |
| Mangosteen Pericarp | 2.69 | 0.686 | 63.3 | 1.17 |  |
| Rose | 0.97 | 0.595 | 65.9 | 0.38 |  |
| Lily | 0.51 | 0.498 | 66.7 | 0.17 |  |
| Coffee | 0.85 | 0.559 | 68.7 | 0.33 |  |
| Broadleaf Holy Leaf | 1.19 | 0.607 | 65.4 | 0.47 |  |
| Hibiscus Sabdariffa L. | 1.63 | 0.40 | 0.57 | 0.37 | [77] |
| Clitoria Ternatea | 0.37 | 0.37 | 0.33 | 0.05 |  |
| Erythrina Variegata | 0.78 | 0.48 | 0.55 | – | [78] |
| Rosa Xanthina | 0.64 | 0.49 | 0.52 | – |  |
| Hibiscus Surattensis | 5.45 | 0.39 | 0.54 | 1.14 | [79] |
| Nerium Olender | 2.46 | 0.40 | 0.59 | 0.59 |  |
| Hibiscus Rosasinesis | 4.04 | 0.40 | 0.63 | 1.02 |  |
| Red Bougainvillea Glabra | 2.34 | 0.26 | 0.74 | 0.45 | [80] |
| Violet Bougainvillea Glabra | 1.86 | 0.23 | 0.71 | 0.31 |  |
| Red Bougainvillea Spectabilis | 2.29 | 0.28 | 0.76 | 0.48 |  |
| Violet Bougainvillea Spectabilis | 1.88 | 0.25 | 0.73 | 0.35 |  |
| Raspberries | 0.26 | 0.42 | 64.8 | 1.50 | [81] |
| Grapes | 0.09 | 0.34 | 61.1 | 0.38 |  |
| Red turnip | 9.50 | 0.425 | 0.37 | 1.7 |  |
| Spinach | 0.47 | 0.55 | 0.51 | 0.13 | [82] |
| Ipomea | 0.91 | 0.54 | 0.56 | 0.28 |  |
| Madder | 0.540 | 0.389 | 0.69 | 0.10 | [83] |
| Khella | 0.384 | 0.437 | 0.47 | 0.05 |  |
| Turmeric | 0.288 | 0.529 | 0.48 | 0.03 |  |
| Bloodleaf | 0.260 | 0.267 | 0.46 | 0.04 |  |
| Alkanet | 0.268 | 0.372 | 0.46 | 0.03 |  |
| Lemon Leaves | 0.286 | 0.539 | 0.74 | 0.05 |  |

Plots of progress in effieciency (η) of DSSC from 1991 to 2014 based on three different types of sensitizers: Ru-based dyes, Metal free dyes and Natural dyes are shown in the Figure 6.

Fig.6 Plots of progress in effieciency (η) of DSSC till date based on three different types of sensitizers: Ru-based dyes, Metal free dyes and Natural dyes

From the graph it can be seen that, there is a steady progress in Ru-based dyes since 1991 and a maximum efficiency of 13 % is achieved in the year 2014 [84]. Metal free dyes on the other hand started its growth from the year 2004. There are several metal free dyes that yield comparable efficiency to that of Ru-based dyes. A maximum of 10.7 % efficiency has been reported in the year 2010 [85]. Finally on considering natural dyes, enormous efforts have been devoted towards improvement in the efficiency of these dyes. A maximum of 1.7 % has been reported in the year 2008 [86]. There are ample of opportunities for further development in regard to the repeatability and reliability of the sensitizers in DSSC for the purpose of commercialization.

4. Recommendations for the improvement of sensitizer stability and efficiency of DSSC

- High stability of the sensitizer can be obtained in a DSSC system by including I− ions as the electron donor to dye cations [87].

- The pigment molecules present in the dye extract should have a shorter distance between the dye skeleton and the point connected to TiO2 surface. This could facilitate better electron transfer from the extract to the TiO2 surface resulting in an increased conversion efficiency of DSSC [15, 79].

- The charge transfer in the TiO2/dye/electrolyte interface resistance leads to a decrease in short circuit current density. Introduction of a functional group and optimization of the dye structure is necessary to improve the efficiency of DSSC [15].

- The controlling the temperature of dye extraction is important in determining the charge-transfer effectiveness of natural dye and thus has a direct impact on the conversion efficiency of DSSC [88].

- Dye aggregation becomes a serious issue that reduces the efficiency of the DSSC. This problem can be avoided by incorporating long alkyl chains and aromatic groups into the dye structure [35].

- Improved charge transfer leading to higher efficiencies can be accomplished with enhanced interaction between TiO2 and dye molecules [70].

- Absorption coefficient of the photosensitizer and the light scattering effect of the semiconductor film improve the IPCE performance in the long wavelength region. Improving the open circuit voltage is also important for realization of higher efficiencies [89].

- Conclusions

In this paper, we reviewed on the status and advances of the different types of sensitizers used in DSSC, including Ru-complex dyes, organic dyes and natural dyes. Ru complexes have shown the good photovoltaic properties such as broad absorption spectrum, suitable excited and ground state energy levels, relatively long excited-state lifetime, and good stability.

It is clear that research into the sensitizers for DSSC is progressing and new Ru-based structures are continue to be reported. Ru-based complexes are considered as best for the production of efficient DSSC having efficiency of 10-11%. But the noble metal Ru is an expensive rare metal and so in order to obtain even cheaper dyes for DSSC, organic photosensitizes and natural dyes are strongly desired.

Ru-free dyes are found to produce excellent conversion efficiencies, which indicate that they are promising candidates for photosensitizers in DSSC. However, the mechanism of dye aggregation is still not fully understood in order to match the performance of Ru complexes. But all the alternatives to Ru-based dyes have so far proved inferior to the Ru dyes.

In summary, DSSC offer a low cost, high efficient option for entry into the commercial market of solar cells. Hence there still remains scope for further development for this technology.

Conflict of Interest

Authors disclose that there is no conflict of interest.

References

- Reagan BO and Grätzel M (1991) A low-cost, high efficiency solar cell based on dye-sensitized colloidal TiO2 films, Nature 353:737-739.

- Hagfeldt A and Grätzel M (2000) Molecular Photovoltaics, Acc Chem Res 33:269-277.

- Ganesan S, Muthuraaman B, Mathew V et al (2008) Performance of a new polymer electrolyte incorporated with diphenylamine in nanocrystalline dye-sensitized solar cell, Sol Energy Mater Sol Cells 92:1718-1722.

- Ragoussi ME, Ince M, Torres T (2013) Recent advances in phthalocyanine-based sensitizers for dye-sensitized solar cells, Eur J Org Chem. doi: 10.1002/ejoc.201301009.

- Zhang Z and Yates JT (2010) Direct observation of surface-mediated electron-hole pair recombination in TiO2 (110), J Phys Chem C 114:3098-3101.

- Raghavan N, Thangavel S, Venugopal G (2015) Enhanced photocatalytic degradation of methylene blue by reduced graphene-oxide/titanium dioxide/zinc oxide ternary nanocomposites, Mat Sci Semicond Proc 30:321-329.

- Ni M, Leung MKH, Leung DYC et al (2007) A review and recent developments in photocatalytic water-splitting using TiO2 for hydrogen production, Renew Sustain Energy Rev 11:401-425.

- Sahoo DD and Roy GS (2013) The effects of Pt doping on the photo-reactivity of TiO2, Researcher 5(1):104-107.

- Nivea R, Gunasekaran V, Kannan R et al (2014) Enhanced photocatalytic efficacy of hetropolyacid pillared TiO2 nanocomposites, J Nanosci Nanotechnol14(6):4383-4386.

- Cheung SH, Nachimuthu P, Joly AG et al (2001) N incorporation and electronic structure in N-doped TiO2 (110) rutile, Surf Sci 601:1754-1762.

- Giribabu L, Kanaparthi RK, Velkannan V (2012) Molecular engineering of sensitizers for dye-sensitized solar cell applications, Chem Rec 12:306-328.

- Zhang S, Yang X, Numata Y et al (2013) Highly efficient dye-sensitized solar cells: progress and future challenges, Energy Environ Sci 6:1443-1464.

- Yella A, Lee HW, Tsao HN et al (2011) Porphyin-Sensitized Solar Cells with Cobalt (II/III)–Based Redox Electrolyte Exceed 12 Percent Efficiency, Science 334:629-634.

- Gokilamani N, Muthukumarasamy N, Thambidurai M et al (2013) Utilization of natural anthocyanin pigments as photosensitizers for dye-sensitized solar cells, J Sol-Gel Sci Technol 66:212-219.

- Narayan MR (2012) Review: Dye sensitized solar cells based on natural photosensitizers, Renew Sustain Energ Rev 16:208-215.

- Gomez-Ortiz NM, Vazquez-Maldonado IA, Perez-Espadas AR et al (2010) Dye-sensitized solar cells with natural dyes extracted from achiote seeds, Sol Energ Mat Sol Cells 94:40-44.

- Al-Ghamdi AA, Gupta RK, Kahol PK et al (2014) Improved solar efficiency by introducing grapheme oxide in purple cabbage dye sensitized TiO2 based solar cell, Solid State Commun 183:56-59.

- Maldonado-Valdivia AI, Galindo EG, Ariza MJ et al (2013) Surfactant influence in the performance of titanium dioxide photoelectrodes for dye-sensitized solar cells, Sol Energ 91:263-272.

- Vougioukalakis GC, Philippopoulos A, Stergiopoulos T et al (2010) Contributions to the development of ruthenium-based sensitizers for dye-sensitized solar cells, Coord Chem Rev doi:10.1016/j.ccr.2010.11.006

- Ito S (2011) Investigation of dyes for dye-sensitized solar cells: ruthenium-complex dyes, metal-free dyes, metal-complex porphyin dyes and natural dyes. In: Kosyachenko LA (eds). InTech, pp 20-48. Available from: http://www.intechopen.com/books/solar-cells-dye-sensitized-devices/investigation-of-dyes-for-dye-sensitizedsolar-cells-ruthenium-complex-dyes-metal-free-dyes-metal-co.

- Luo P, Niu H, Zheng G et al (2009) From salmon pink to blue natural sensitizers for solar cells: Canna indica L, Salvia splendens, cowberry and Solanum nigrum L, Spectrochim Acta Part A:Mol Biomol Spectrosc 74:936-942.

- Hemalatha KV, Karthick SN, Justin Raj C et al (2012) Performance of kerria japonica and rosa chinensis flower dyes as sensitizers for dye-sensitized solar cells, Spectrochim Acta Part A: Mol Biomol Spectrosc 96:305-309.

- Ludin NA, Al-Alwani Mahmoud AM, Mohamad AB et al (2014) Review on the development of natural dye photosensitizer for dye sensitized solar cells, Renew Sustain Energ Rev 31:386-396.

- Longo C and De Paoli MA (2003) Dye-sensitized solar cells: a successful combination of materials, J Braz Chem Soc. Doi:org/10.1590/S0103-50532003000600005.

- Mehmood U, Rahman S, Harrabi K et al (2014) Recent advances in dye sensitized solar cells, Adv Mater Sci Engg. Doi:org/10.1155/2014/974782.

- http://shodhganga.inflibnet.ac.in/bitstream/10603/3917/10/10_chapter%201.pdf

- Zakerhamidi MS, Ghanadzadeh A, Moghadam M (2012) solvent effects on the UV/visible absorption spectra of some aminoazobenzene dyes, Chem Sci Trans 1:1-8.

- Banerjee A, Shuai Y, Dixit R et al (2010) Concentration dependence of fluorescence signal in a micro fluidic fluorescence detector, J Luminescence 130:1095-1100.

- Fattori A (2010) Electrochemical and spectroelectrochemical studies of dyes used in dye-sensitized solar cells. PhD Dissertation, University of Bath.

- Gratzel M (2005) Solar energy conversion by dye-sensitized photovoltaic cells, Inorg Chem 44:6841-6851.

- Gratzel M (2006) Photovoltaic performance and long-term stability of dye-sensitized meosocopic solar cells, Comptes Rendus Chimie 9:578-583.

- Evans RC, Douglas P, Burrow HD (2013) Applied Photochemistry. Springer, New York.

- Thavasi V, Renugopalakrishnan V, Jose R et al (2009) Controlled electron injection and transport at materials interfaces in dye sensitized solar cells, Mater Sci Engg R 63:81-99.

- Wang Y, Matsushima T, Murata H et al (2012) Molecular order, charge injection efficiency and the role of intramolecular polar bonds at organic/organic heterointerfaces, Org Electron 13:1853-1858.

- Pastore M, Selloni A, Fantacci S et al (2014) Electronic and Optical Properties of Dye-Sensitized TiO2 Interfaces, Top Curr Chem doi:10.1007/128_2013_507.

- Sá J, Friedli P,   Geiger R et al (2013) Transient mid-IR study of electron dynamics in TiO2 conduction band, Analyst 138:1966-1970.

- http://www.wiley-vch.de/books/sample/3527329684_c01.pdf

- http://k2.chem.uh.edu/preprints/ParisProceedings.pdf

- Mohammadi N, Mahon PJ, Wang (2012) Toward rational design of organic dye sensitized solar cells (DSSC): an application to the TA-St-CA dye, J Mol Graphics Model. doi:10.1016/j.jmgm.2012.12.005.

- Rack JJ and Gray HB (1999) Spectroscopy and electrochemistry of mer-RuCl3 (dmso) (tmen)]dimethylsulfoxide is sulfur-bonded to Ru(II), Ru(III),and Ru(IV), Inorg Chem 38:2-3.

- Taube H (1999) Electron transfer between metal complexe-a retrospective view, Angew Chem Int Ed Eng 23:329-334.

- Nazeruddin MK, Kay A, Podicio I et al (1993) Conversion of light to electricity by cis‐X2 bis(2,2′‐bipyridyl‐4,4′‐dicarboxylate)ruthenium(II) charge‐transfer sensitizers (X = Cl−, Br−, I−, CN−, and SCN−) on nanocrystalline titanium dioxide electrodes, J Am Chem Soc 115:6382-6390.

- Nazeeruddin MK, Angelis FD, Fantacci S et al (2005) Combined experimental and DFT-TDDFT computational study of photoelectrochemical cell ruthenium sensitizers, J Am Chem Soc 127:16835-16847.

- Sekar N and Gehlot VY (2010) Metal complex dyes for dye-sensitized solar cells: recent developments, Resonance 819-831.

- Lattante S (2014) Electron and hole transport layers: their use in inverted bulk heterojunction polymer solar cells, Electronics. doi: 10.3390/electronics3010132.

- Shelke RS, Thombre SB, Patrikar SR (2013) Status and perspectives of dyes used in dye sensitized solar cells, Int J Ren Energ Res 3:12-19.

- Park SS, Won YS, Choi YC et al (2009) Molecular design of organic dyes with double electron acceptor for dye-sensitized solar cell, Energ Fuel 23 (7):3732-3736.

- Oyama Y, Harima Y (2009) Molecular designs and syntheses of organic dyes for dye-sensitized solar cells, Eur J Org Chem 18:2903-2934.

- Pastore M and Angelis FD (2010) Aggregation of organic dyes on TiO2 in dye-sensitized solar cells models: an ab initio investigation, ACS Nano 4:556-562.

- Kay M and Grätzel M (1996) Low cost photovoltaic modules based on dye sensitized nanocrystalline titanium dioxide and carbon powder, Sol Energ Mater Sol Cell 44 (1):99-117.

- http://en.wikipedia.org/wiki/Indole.

- Horiuchi T, Miura H, Uchida S (2003) Highly-efficient metal-free organic dyes for dye-sensitized solar cells, Chem Comm 24:3036-3037.

- Li B, Wang L, Kang B et al (2005) Review of recent progress in solid state dye-sensitized solar cells, J Sol Energ Mater Sol Cell 90:549-573.

- Lu S, Koeppe L, Gunes R et al (2007) Quasi-solid state dye-sensitized solar cells with cyanoacrylate as electrolyte matrix, J Sol Energ Mater Sol Cell 91:1081-1086.

- Wang G and Lin Y (2009) Performance characteristics of dye sensitized solar cells with counter electrodes based on nip-plated glass and titanium plate, Curr Appl Phy 9:1005-1008.

- Wang ZS, Kawauchi H, Kashima T et al (2004) Significant influence of TiO2 photo electrode morphology on the energy conversion efficiency of N719 dye-sanitized solar cell, J Coord Chem Rev 248: 381-1390.

- Arakawa H, Yamaguchi T, Okada K et al (2009) Highly durable dye-sensitized solar cells, J Fujikura Tech Rev 55-60.

- Yang HX, Huang ML, Wu JH et al (2003) The polymer gel electrolyte based on poly (methyl methacrylate) and its application in quasi-solid-state dye sensitized solar cell, J Mater Chem Phy 110:38-42.

- Weon-Piltai (2003) Photoelectrochemical Properties of ruthenium dye-sensitized nanocrystalline SnO2:TiO2 solar cells, J Sol Energ Mater Sol Cell 76:65-73.

- Bandaranayake PKM, Jayaweera PVV, Tennakone K (2003) Dye-sensitization of magnesium-oxide-coated cadmium sulfide, J Sol Energ Mater Sol Cell 76:57-64.

- Hasinm PS, Hasin P, Alpuche-Aviles MA et al (2009) Mesoporous Nb - doped TiO2 as pt support for counter electrode in dye sensitized solar cells, J Phy Chem 113:7456-7460.

- Hara K, Tachibana Y, Ohga Y et al (2003) Dye-sensitized nanocrystalline TiO2 solar cells based on novel coumarin dyes Sol Energ Mater Sol Cells 77:89-103.

- Lee CW, Lu HP, Lan CM et al (2009) Novel zinc porphyin sensitizers for dye-sensitized solar cells: synthesis and spectral, electrochemical, and photovoltaic properties, Chem Eur J 15:1403-1412.

- Wu Y, Marszalek M, Zakeeruddin SM et al (2012) High-conversion-efficiency organic dye-sensitized solar cells: molecular engineering on D–A–π-A featured organic indoline dyes, Energ Environ Sci 5:8261-8272.

- Chang H, Lo YJ (2010) Pomegranate leaves and mulberry fruit as natural sensitizers for dye-sensitized solar cells, Sol energ 84:1833-1837.

- Davies KM (2004) Plant pigments and their manipulation 14th edn. USA:Blackwell publishing Ltd

- Kumara NTRN, Ekanayake P, Lim A et al (2013) Layered co-sensitization for enhancement of conversion efficiency of natural dye sensitized solar cells, J Alloys Compd 581:186-191.

- Wang XF, Xiang J, Wang P, Koyama Y (2005) Dye-sensitized solar cells using chlorophyll a derivate as the sensitizer and carotenoids having different conjugation lengths as redox spacers, Chem Phys Lett 408:409-414.

- Scheer HI (2003) Light-harvesting antennas in photosynthesis. In: Green BR and Parson WW (eds). Dordrecht: Kluwer Academic Publishers. pp 513-530.

- Narayan M and Raturi A (2011) Investigation of some common fijian flower dyes as photosensitizers for dye sensitized solar cells abstract, Appl Sol Energ 47:112-117.

- Vargas FD, Jiménez AR, López OP (2000) Natural pigments: carotenoids, anthocyanins, and betalains-characteristics, biosynthesis, processing, and stability, Crit rev food sci nutrition 40:173-289.

- Brouillard R, Dangles O, Jay M et al (1993) Polyphenols and pigmentation in plants. Polyphenolic Phenomena Paris: INRA. pp 41-47.

- Swain T and Bate-Smith EC (1962) Flavonoid compounds. In: Florkin M, Mason HS (eds). Comparative Biochemistry Vol. III:Constituents of Life. Part A, New York, Academic Press. pp 755-809.

- Steyn WJ, Wand SJE, Holcroft DM et al (2002) Anthocyanins in vegetative tissues: a proposed unified function in photoprotection, New Phytologist 155:349-361.

- Goodwin TW and Britton G (1988) Distribution and analysis of carotenoids. In: Goodwin TW (eds). Plant Pigments, London: Academic Press. pp 62-132.

- Huizhi Z, Wu L, Gao Y et al (2011) Dye-sensitized solar cells using 20 natural dyes as sensitizers, J Photochem Photobiol A Chem 219:188-194.

- Grünwald R and Tributsch H (1997) Mechanisms of instability in Ru-based dye sensitized solar cells, J Phys Chem 101:2564-2575.

- Hao S, Wu J, Huang Y, Lin J. Natural dyes as photosensitizers for dye-sensitized solar cell. Sol Energ 2006; 80:209-14.

- Wongcharee K, Meeyoo V, Chavadej S (2007) Dye-sensitized solar cell using natural dyes extracted from rosella and blue pea flowers, J Sol Energ Mater Sol Cell 91:566-571.

- Hemandez-Martinez AR, Vargas S, Estevez M et al (2012) Dye sensitized solar cells from extracted bracts bougainvillea betalain pigments. First International Congress on Instrumentation and Applied Sciences 10:1-15.

- Alhamed M, Issa AS, Doubal AW (2012) Studying of natural dyes properties as photo-sensitizer for dye sensitized solar cells (DSSC), J Electron Devices 16:1370-1383.

- Chang H, Wu HM, Chen TL et al (2010) Dye sensitized solar cell using natural dyes extracted from spinach and ipomoea, J Alloys Compd 495:606-610.

- Moustafa KF, Rekaby M, El Shenawy ET et al (2012) Green dyes as photosensitizers for dye-sensitized solar cells, J Appl Sci Res 8:4393-4404.

- Mathew S, Yella A, Gao P et al (2014) Dye-sensitized solar cells with 13% efficiency achieved through the molecular engineering of porphyin sensitizers, Nature Chem 6:242-247.

- Zhou N, Prabakaran K, Lee B et al (2015) Metal-free tetrathienoacene sensitizers for high-performance dye-sensitized solar cells, J Am Chem Soc 137(13):4414-4423.

- Calogero G, Marco GD, Cazzanti S et al (2010) Efficient dye-sensitized solar cells using red turnip and purple wild sicilian prickly pear fruits, Int J Mol Sci 11(1):254-267.

- Hara K, Arakawa H, Luque A et al (2005) Handbook of photovoltaic science and engineering. John Wiley & Sons Ltd.  doi: 10.1002/0470014008.ch15.

- Shibl HM, Hafez HS, Rifai RI et al (2013) Environmental friendly, low cost quasi solid state dye sensitized solar cell: polymer electrolyte introduction, J Inorg Organomet Polym 23:944-949.

- Abdou EM, Hafez HS, Bakir E et al (2013) Photostability of low cost dye-sensitized solar cells based on natural and synthetic dyes, Spectrochim Acta Part A:Mol Biomol Spectrosc 115:202-207.